Ion Induced Millimeter-Size Structures Formation on Tungsten Surface

Balkova Y.B., Myroshnyk M.O., (Senior Researcher Girka O.I.)

Іонно-стимульоване формування структур міліметрового розміру на поверхні вольфраму

Балькова Ю.Б., Мирошник М.О., (ст.н.с. Гірка О.І.)

School of Physics and Technologies, V.N. Karazin Kharkiv National University, 
4 Svobody Sq., Kharkiv, 61022, Ukraine

oleksiigirka@karazin.ua

The presence of impurities will influence the PWI processes by both physical and chemical interactions. Tungsten, beryllium, helium and divertor cooling species (argon, neon, or nitrogen) will be present as impurities in the ITER plasma [1]. Polished tungsten sample with purity 99.99% wt. has been exposed to Ar ion beam generated by FALCON ion source [2]. Typical parameters during steady-state expose were the following: Ar ion flux was 2-3×1022 m-2s-1, heat flux was about 3 MW m-2, average ion energy of 2 keV and the ion fluence reaches 1027 m-2. Sample temperature was modelled and measured with thermocouple [3-4]. During the exposures, the temperature of sample is more than 1000 K. Following the exposure, SEM study revealed that surface is populated with castle-like structures with density of 2-3 features per mm2. Their shape is distinguished by high height-to-diameter aspect ratio and pronounced asymmetry. Typical height of the structures exceeds what has been reported in the literature (1-100 um) and reaches 0.3-0.4 mm. Surface activated diffusion considered to be as primary mechanism of structures growth, which can be prevented by a presence of surface stresses [5].

## References

- Ch. Linsmeier, B. Unterberg, J.W. Coenen, R.P. Doerner, H. Greuner, A. Kreter, J. Linke and H. Maier. Material testing facilities and programs for plasma-facing component testing. Nucl. Fusion 57 (2017) 092012 (34pp). https://doi.org/10.1088/1741-4326/aa4feb

- O. Girka, I. Bizyukov, K. Sereda, A. Bizyukov, M. Gutkin, V. Sleptsov. Compact steady-state and high-flux FALCON ion source for tests of plasma-facing materials. Review of Scientific Instruments, 83 (2012), 083501

- O. Girka, O. Bizyukov, S. Bogatyrenko, I. Bizyukov. Aluminium Surface Morphology Behaviour under High-Flux Helium Ion Bombardment. Nuclear Instruments and Methods in Physics Research B, 405 (2017), p. 31–35.

- S.S. Herashchenko, V.A. Makhlaj, O.I. Girka, N.N. Aksenov, I.A. Bizyukov, S.V. Malykhin, S.V. Surovitskiy, K.N. Sereda, A.A. Bizyukov. Erosion Features of Tungsten Surfaces under Combined Steady-State and Transient Plasma Loads. Problems of Atomic Science and Technology. 2016, № 6. Series: Plasma Physics (22), p. 69-72.

- V.V. Bobkov, S.S. Alimov, Vl.V. Bobkov, Yu.V. Slyusarenko, R.I. Starovoitov. Growth of metal newborn formations on cathode surface under influence of plasma flow. Surface and Coatings Technology 174 –175 (2003) 1271–1275.