Aluminium and Titanium Alloys Surface Behaviour

under Argon and Helium Ion Exposure

Myroshnyk1 M., (Senior Researcher Girka1 O., Professor Kaczmarek2 Ł.)

Поведінка поверхонь алюмінієвих та титанових сплавів під дією опромінення іонами аргону та гелію

Мирошник М.О., (ст.н.с. Гірка О.І., проф.. Качмарек Л.)

1School of Physics and Technologies, V.N. Karazin Kharkiv National University, 
4 Svobody Sq., Kharkiv, 61022, Ukraine

2Institute of Materials Science and Engineering, Lodz University of Technology, Stefanowskiego 1/15, 90-924, Lodz, Poland

oleksiigirka@karazin.ua

Surface topography changes due to ion bombardment are the basis for a number of materials applications involving optical absorption, surface analysis, nuclear reactor walls, biological implants and adhesive bonding [1]. The surface roughness is a very important parameter, which is considered in preparation of specimens for TEM and biological implant materials [2-4]. Hillocked layer is required part of biocompatible electrodes manufacturing process [5]. Surface features and cone-like structures growth under exposure of ion flux was studied previously [6-7].

Samples of Aluminium alloy Al(2024) and Titanium alloy Ti-6Al-4V are irradiated with 2 keV Helium and Argon ion fluxes using FALCON ion source. Cone-like structures are found to be formed on the surface of two Al(2024) samples due to both irradiation conditions: Argon and Helium exposure reaching total charge 150 C per sample. Argon exposure of Ti-6Al-4V causes cones formation unlike second case: Helium exposure causes only physical sputtering morphology at the same total charge. Chemical composition of grown structures is obtained from Energy Dispersive Spectroscopy (EDS). Surface roughness and roughness profile are investigated with Confocal Microscope. Hardness of irradiated surfaces is obtained from results of whiskers hardness test. Residual stresses after irradiation and phase composition are investigated by X-ray Diffraction spectroscopy (XRD). Free surface energy measured with drop test.

## References

- R. Messier, S.V. Krishnaswamy, P.L. Walker. Ion Bombardment Induced Cone Formation on Glassy Carbon and Graphite Surfaces. Carbon, 1982, Vol. 20, No. 1, pp. 29-33. https://doi.org/10.1016/0008-6223(82)90070-7

- Z.W. Kowalski. Influence of the-ion incidence angle of alumina surface cleanness, roughness and topography. Journal of Materials Science, Vol. 17, 1982, p. 1627-1631. https://doi.org/10.1007/BF00540788

- B.A. Banks, A.J. Weigand, C.A. Babbush, C.L. Van Kampen. Potential Biomedical Applications of Ion Beam Technology. NASA Technical Memorandum (NASA TM X-73512), 1976, Florida: Twelfth International Electric Propulsion Conference. https://ntrs.nasa.gov/search.jsp?R=19770030155

- M.A. de Maeztu, J.I. Alava, C. Gay-Escoda. Ion implantation: surface treatment for improving the bone integration of titanium and Ti-6Al-4V dental implants. Clin Oral Implants Res. 2003 14 (1):57-62.

- J.S. Wollam. Method of making biocompatible electrodes. US5118400 A, 1992

- V.V. Bobkov, S.S. Alimov, Vl.V. Bobkov, Yu.V. Slyusarenko, R.I. Starovoitov. Growth of metal newborn formations on cathode surface under influence of plasma flow. Surface and Coatings Technology 174 –175 (2003) 1271–1275. http://dx.doi.org/10.1016/S0257-8972(03)00631-5

- O. Girka, O. Bizyukov, S. Bogatyrenko, I. Bizyukov. Aluminium Surface Morphology Behaviour under High-Flux Helium Ion Bombardment. Nuclear Instruments and Methods in Physics Research B, 405 (2017), p. 31–35. http://dx.doi.org/10.1016/j.nimb.2017.05.019